SPECIFICATION SHEET NO: **NW361**

\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_

**NEW WORK/REPAINT:** NEW WORK – INTERIOR

\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_

**SUBSTRATE:** Wood

**\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_**

**PAINT FINISH:** Plascon Glatex 8 - Solid Colour PRODUCT CODE: **PL 17**

(Smooth, highly durable 2-pack polyurethane gloss enamel)

 **\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_**

**COLOUR:** White only.

**\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_**

**ENVIRONMENT: The Maintenance Cycle is a guide but can vary due to micro-climate changes identified on the site which will affect the longevity of the coating system**

As per ISO 12944-2:1998 Maintenance Cycle (Years)

 C1 - Inland 10

C3 - Industrial 10

 C5 - Coastal / Marine 10

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| **Plascon Coating System** | **Application****Method** | **Spreading****Rate** **m²/ℓ** | **WFT/DFT µm****(min & max)** | **Reducer/****Cleaner** | **Overcoating time****h @ 23 °C** | **Technical Data Sheet No** | **TVOC****g/ℓ** |
| **Primer**Plascoguard 40 Universal Epoxy Primer(PEX 40/PEH 40)**Mixing ratio:** **4:1 by volume** | B, R or S | @ 45 µmTheo: 8.9 Prac: 5.2 | WFT 100 -125 DFT 40-50 | EPT 2 | 4 | PEX 40 | 394 |
| **1st Finishing Coat**Plascon Glatex 8 (PL 17)**Mixing ratio****3:1 by volume**  | B, R, S | @ 30 µmTheo: 12Prac: 6.6 | WFT 69- 97 DFT 25-35 | Glatex 8Thinner (PT 1) | 16 | PL | 365 white |
| **2nd Finishing Coat**Plascon Glatex 8 (PL 17)**Mixing ratio****3:1 by volume**  | B, R, S | @ 30 µmTheo: 12Prac: 6,6 | WFT 69- 97 DFT 25-35 | Glatex 8Thinner (PT 1) | 16 | PL | 365 white |

SPECIFICATION SHEET NO: **NW361**

\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_

**SURFACE PREPARATION:**

* Machine sand floors in direction of the grain to remove surface coatings or contaminants until a smooth and uniformly clean profile is obtained.
* Rake out open joints to remove dirt and wax polish contaminants. Vacuum floor.
* Just before coating, wipe surface with mutton cloth dampened with Universal Reducer (PUR 1) to ensure a spotlessly clean and dust free surface.

**\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_**

**APPLICATION:**

**Primer Coat**

Mix base and hardener thoroughly in a 4:1 ratio by volume before use.

* Apply one coat of Plascoguard 40 Universal Epoxy Primer (PEX 40/PEH 40) to achieve a continuous film. Allow 4 hours to dry.

**Finishing Coats**

**Mixing:**

Mix base and hardener thoroughly in a 3:1 ratio by volume before use.

Do not thin more that 5% with PT 1 Thinner.

* Apply two full coats of Plascon Glatex 8 (PL 17) to achieve complete obliteration, allowing 16 hours drying between coats.

**\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_**

**TABLE REFERENCES:**

* Technical Data Sheet (TDS): User must always ensure that latest issue is used.
* B = Brush (ready for use), R = Roller (synthetic, min. 10mm pile) (ready for use), S = Airless spray (ready for use).
* Theoretical spreading rate quoted is for smooth non-porous substrates and does not include allowance for surface profile, porosity, wastage and uneven film application. Suitable allowance should be made according to type of work, method and skill of applicator. Practical spreading rate quoted is an average guide only - actual must be determined by user.
* Overcoating times are at 23 °C and 75 % relative humidity. Longer times must be allowed under cooler and moist conditions. DO NOT paint during inclement weather and when temperature is below 10 °C.
* Fading and chalking will occur to a greater or lesser degree depending on pigmentation and generic binder type.
* NB: Life expectancy may vary, depending on environmental conditions and stresses, within the macro/micro climate of the project.

Copyright @Kansai Plascon (Pty) Ltd 2013. All rights reserved. No part of this work may in any form or by any means be reproduced without prior written permission of the copyright owner. PLASCON is the registered trade mark of Kansai Plascon (Pty) Ltd,

**\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_**